## Slide 1: DOE-NNSA Massie Chair Program Activities at Tuskegee University
Nosa O. Egiebor
DOE/NNSA-Samuel P. Massie Chair
Chemical Engineering Department
Tuskegee University
Tuskegee, AL 36088

## Slide 2: Current Massie Chair Team at Tuskegee University
Research Faculty:
  Dr. Tarig Hassan – Research Asst. Professor
Students:
  Freddie Eskridge - Undergrad
  Timothy Powel - Undergrad
  Valerie Gordon - Undergrad
  Derrick Pattaway - Undergrad
  Samuel Gana - Graduate (PhD)
  Mishu Khan - Graduate (MS)
Faculty Collaborators:
  Dr. Jonathan Mbah – Chemical Engineering
  Dr. Shamim Begum – Chemical Engineering
  Dr. Sesha Srinivasan – Physics

## Slide 3: Massie Chair Program Activities at Tuskegee University
Research
  Development of corrosion & degradation resistant materials (metallic alloys) for Generation IV nuclear reactors.
Education
  Graduate students’ education and research training
  Undergraduate education, and the integration of research into undergraduate training.
Outreach & Partnership
  High school science teacher mentorship & Summer training for Grades 10 & 11 high school students
  Summer internship for undergraduate students
  National & international partnerships for STEM research & education
    Africa-US Higher Education Initiative in STEM (USAID)

## Slide 4: Research - Introduction
New DOE-NNSA Nuclear Energy Initiative  Development of Generation IV Nuclear Energy Systems
These next generation nuclear plants (based on the Energy Policy Act of 2005), include:
    Very High Temperature Reactor (VHTR).
      Up to 950oC output temperatures
      Gas cooled (Helium, CO2, etc.)
    Sodium Fast Reactor (SFR).
      500 – 550oC
      Liquid sodium cooled

## Slide 5: Schematics of VHTR Gen. IV Reactor

## Slide 6: Introduction (contd.)
Advantages of the Generation IV Nuclear Reactors
  Improved safety and reliability.
  Sustainability & Cost effectiveness.
  Significant proliferation resistance.
  Hydrogen production through high temperature electrolysis of water.
  Deep-Burn capability  Significantly reduced high-level waste generation.
  Implementation in 2011-2021 time frame.

## Slide 7: Research Needs of Gen. IV Reactor Development
Critical R & D Needs:
  Development and evaluation of materials for use in Generation IV nuclear reactors under high temperatures and pressure
  Behavior of high-temperature gas reactor fuels
  Design methods development & validation
  Hydrogen production technologies
  Energy conversion processes

## Slide 8: Tuskegee Research Objectives
Study the effect of high service temperatures (500o – 1000oC) on the nanostructure and phase transformation behaviors of predetermined compositions of ferritic steel, oxide dispersion strengthened steel (ODS), and nickel-based alloys as candidate materials for Generation IV reactor systems.
Investigate how alloy compositions affect surface corrosion behavior, particularly the initiation of stress corrosion cracking (SCC).
Evaluate the effect of elevated temperatures and pressures, and helium-coolant hydrodynamics on the corrosion behavior of ferritic steel, nickel steel, and ODS candidate steel samples.
Investigate the effect of aging and extended reaction times (6 – 24 months) under high temperatures on the corrosion response of Ferritic, ODS, and nickel-based alloy samples.

## Slide 9: Our Previous Research Approach (Grant Period 2005-2010)
Obtain candidate metallic alloys of various compositions from commercial suppliers.
Subject the samples to severe service conditions of high temperatures & pressure.
Study the impact of severe conditions on micro-structural evolution such as Cr surface segregation.
Evaluate the corrosion resistance and physical stability of the treated samples using electrochemical impedance spectroscopy (EIS).
      Problem  We had difficulties finding suppliers for the needed compositions of the candidate alloys needed.

## Slide 10: Current Research Approach
Produce the materials in our lab  Produce Oxide Dispersion Strengthened (ODS) steel and Fe-Cr alloys by Mechanical Alloying (MA) from powders.
Hot press the powdered alloys to sheets for evaluation
Evaluate and characterize the alloys in terms of microstructure, physical and mechanical properties.
Determination of corrosion and degradation resistance at elevated temperatures & coolant hydrodynamics.

## Slide 11: Mechanical Alloying (MA) e.g. ODS Alloy Production
Step 1. Ball milling of pure powders of the constituents, e.g Fe, Ti, Al, & Yttria (Y2O3) to form oxide dispersion strengthened (ODS) alloy
      Form sub-micron particles of alloys (nanomaterials)

## Slide 12: Step 1. (Contd.) Ball Mill Operating Principles
Feed material: < 4 mm powders Final fineness*: < 1 µm, for colloidal grinding < 0.1 µm
1. Milling/grinding, 2. mechanical alloying, 3. nano-structure development, 4. reactive bonding

## Slide 13: Step 2 (MA)  High Temperature Press to Form Flat Alloy Sheets (45 tons)

## Slide 14: Step 3: Study of Corrosion Resistance & Physical Stability at High Temps
3-Electrode Potentiostat for Electrochemical Impedance Spectroscopy (EIS)

## Slide 15: Outreach & New Partnership  Africa-US Higher Education STEM Initiative
Tuskegee University – Massie Chair program partnering with:
  International Institute for Water & Environmental Engineering (2iE) in Burkina Faso
  University of Mines & Technology (UMaT) in Ghana
  University of Benin, Benin City, Nigeria
  USAID/Higher Education for Development (HED)
  Awarded $1.1 million for 2010 – 2012 as initial implementation grant from USAID

## Slide 16: Minority STEM Capacity Development Impact
Annual Impacts:
  20 – 30 undergraduate students receive tutorship annually
  5 – 8 undergraduate students are engaged each year for direct laboratory research training.
  5 High school students are involved in summer training per year
  3 MS & PhD graduate students per year
  1 Postdoctoral Research Fellow
  3 Junior faculty members are mentored

## Slide 17: THANK YOU!!
QUESTIONS Please?